Magnet Challenge – Update 2023-06-29

---
Implementing Stenglein approach

---
Implementing Stenglein model
- Part 1: quasistatic hyst. Losses
- Part 2: effective frequency depending on slopes

---
Using stenglein model without own measurements
- Stenglein model fits its own measurements
- But not the datasheet measurements
- Datasheet values are lower than in stenglein measurement
- For accurate results, measurement on every batch necessary
Solid: Datasheet
Dashed: Stenglein-Model
Stars: Stenglein measurements

---
Part 1: Getting quasistatic hysteresis factors
DC-part
Magnet loss data
DC-part

---
Part 2: Rate dependent data

---
Drawbacks
- Model only valid for a single temperature. Curve fitting for several temperatures can be done
- The quasistatic hysteresis loss needs measurments < 1 kHz. Stenglein uses 100 Hz for measurements
- Model requires own measurements, the datasheet does not contain enough data